IMPACT OF MOLECULAR WEIGHT ON 
MATERIAL PROPERTIES

Normalize for different monomers by comparing DP

Degree of Polymerization = D. P.

Molecular Weight (Mn)

=

Molecular weight of Monomer (Mo)

Vinyl Monomers

| X | Polymer | Abbreviation |
| --- | --- | --- |
| H | Polyethylene | PE |
| CH3 | Polypropylene | PP |
| Cl | Poly(vinyl chloride) | PVC |
| Phenyl | Polystyrene | PSt |
| CN | Polyacrylonitrile | PAN |
| COOCH3 | Poly(methyl acrylate) | PMA |
| O-COCH3 | Poly(vinyl acetate) | PVAc |

Vinylidene Monomers

| X | Y | Polymer | Abbreviation |
| --- | --- | --- | --- |
| CH3 | CH3 | Polyisobutylene | PIB |
| Cl | Cl | Poly(vinylidene chloride) | PVDC |
| F | F | Poly(vinylidene fluoride) | PVDF |
| Phenyl | CH3 | Poly((-methyl styrene |  |
| CH3 | COOCH3 | Poly(methyl methacrylate) | PMMA |
| CN | COOR | Poly(alkyl (-cyanoacrylate |  |

### Structural Complexity of Polymers

Molecular Level

Homopolymers

Head to Tail vs. Head to Head Adducts

1,2- vs 1,4 Adducts

Tacticity of Enchainments

Branching

Copolymers

Identity and Number of Comonomers

Ratio and Distribution of Comonomers

Statistical

Alternating

Blocks

## Grafts

Molecular Weight      Mn, Mw, Mz, Mv   Averages

Molecular Weight Distribution

Crosslinking

Density

Length of Crosslinks

Morphology

Impurities

Additives

Structural Complexity of Polymers

Time Dependent Changes

Chemical Reactions

Hydrolysis

Dehydrohalogenation

Photodegradation

Oxidation

Thermal Degradation

Processing

Aging

Crystallization

Changes in Polymorphism

Weathering

Plasticizer Loss -- Imbrittlement

Microscopic (Intermolecular Interactions)

Chain entanglement --amorphous

Chain ordering--liquid crystalline

Crystallinity

Phase separations (microdomains)

Morphology

Types of Intermolecular Forces

| Type of Force | Relative Strength | Low Molecular Analog | Polymer |
| --- | --- | --- | --- |
| Dispersion or Van der Waals | Weak | Methane Hexane | Polyethylene Polypropylene |
| Dipole-Dipole | Medium | CH3Cl CH3CO2CH3 | PVC PMMA |
| Hydrogen bonding | Strong | H2O CH3CONH2 | Proteins Cellulose Polyamide |
| Electrostatic or Ionic | Very Strong | NaCl CH3CO2-Na+ | Ionomers |

# Macroscopic Properties (Physical Behavior)

Tensile and/or Compressive Strength

Elasticity

Toughness

Thermal Stability

Flammability and Flame Resistance

Degradability

Solvent Resistance

Permeability

Ductility  (Melt Flow)

Surface Texture - - Morphology

Electrical and Optical Properties

Tacticity

#### Isotactic

#### All asymmetric carbons have same configuration

Methylene hydrogens are meso

Polymer forms helix to minimize substituent interaction

Syndiotactic

#### Asymmetric carbons have alternate configuration

Methylene hydrogens are racemic

Polymer stays in planar zig-zag conformation

Heterotactic    (Atactic)

#### Asymmetric carbons have alternate configuration

# GLASS TRANSITION, Tg

Definition:  The onset of seqmental motion of seqments with 				40-50 carbons atoms

Physical Change   Expansion of volume

Free volume required to allow segmental motion

Properties Affected

Specific Volume / Density

Specific Heat, Cp

Refractive Index

Modulus

Dielectric Constant

Permeability

# Tg is an approximation

Depends upon measurement technique

Depends upon molecular weight

Polystyrene MW = 4000		Tg = 40(C

= 300,000	      = 100(

# FACTORS INFLUENCING Tg

Tg is proportional to Rotational Freedom

For symmetrical polymers  	Tg, / Tm in (K ( 1/2

unsymmetical polymers				  ( 2/3

# 1. Chain flexibility

Silicone ( Ether ( Hydrocarbon ( Cyclic HC ( Aromatics

# 2. Steric Bulk of Substituents

Tg = -120(C		    5(C		  -24(C		  -50(C

Long side chains may act as plasticizers (C ( 6)

Tg = 	  -55(C			     88(C

Tg =  5(C		   100(C		     150(C

# 3. Molecular Symmetry

Asymmetry increases chain stiffness.

# 4. Polar Interactions increase Tg

Hydrogen bonding

# 5. Molecular Weight up to Critical Limit

# 6. Crosslinking

Reduces Segment Mobility

# FACTORS INFLUENCING Tm

# 1.	Chain flexibility

Silicone ( Ether ( Hydrocarbon ( Cyclic HC ( Aromatics

# 2.	Substituents Producing Lateral Dipoles

Hydrogen bonding

# 3. 	Molecular Symmetry

Symmetry allows close packing

# 4. 	No Bulky Substituents to Disrupt Lattice if placement is Random

# 5.	Structural Regularity

monomer placement

head to tail

1,2- vs 1,4-

1,2- vs 1,3- vs 1,4- aromatic substitution

geometric isomers of enchainments

cis or trans -C=C-;  cyclic ring

tacticity

# FACTORS REQUIRED TO PROMOTE CRYSTALLIZATION

# Thermodynamic

1.  Symmetrical chains which allow regular close packing in crystallite

2.  Functional groups which encourage strong intermolecular attraction to stabilize ordered alignment.

# Kinetic

1. Sufficient mobility to allow chain disentanglement and ultimate alignment

Optimum range for mobility

TM  -10(  (  Tg  + 30(

at TM  segmental motion too high

at Tg  viscosity too high

2. Concentration of nuclei

concentration of nucleating agents

thermal history of sample

Factors Controlling Morphology

Molecular Structure

(Monomer units, microstructures, molecular weight)

Conformation of
Single chain

Molecular Interactions

Rubberlike
Elasticity

Crystallite Formation

Glass Formation

% Crystallinity

Mechanical and Thermal Properties

Morphology

PROPERTIES INFLUENCED BY MORPHOLOGY

| Crystalline Domain | Amorphous Defects |
| --- | --- |
| Density |  |
| Specific Heat | Permeability |
| Elastic Modulus | % Elongation |
| Tensile Strength | Impact Strength |
| Melting Point | Glass Transition |
| Opacity | Optical Clarity |
| Solvent Resistance | Solubility |

THERMAL BEHAVIOR OF POLYMERS

| Amorphous | Crystalline | Liquid Crystalline |
| --- | --- | --- |
| Liquid | Liquid | Isotropic Liquid |
|  | ( Tm | ( Tm |
| Gum |  | "Ordered Liquid |
|  | Flexible Thermoplastic | ( Tlc |
| Rubber |  | Flexible Thermoplastic |
| ( Tg | ( Tg | ( Tg |
| Glass | Crystalline and glassy domains | Crystalline and glassy domains |

# CLASSIFICATION OF POLYMERS BY PROPERTIES

| Property | Elastomer | Plastic | Fiber |
| --- | --- | --- | --- |
| Morphology | Amorphous | Amorphous glass | Crystalline |
| Use Temp. | 20( C above Tg | Below Tg and Tm | Below Tm |
| Initial Modulus | Low | Moderate | High |
| E, psi | 15-150 | 1500-200,000 | 150,000 -1,500,000 |
| Tensile Strength | Low | Moderate | High |
| Elongation | High | Moderate | Low |
| L/Lo, % | 100-1000 | 20-100 | ( 20 |
| Tg | Low (-100 ( -50(C | High (( 70( C) | Moderate |
| Tm | Low (( 35(C) | Moderate | High (( 250(C) |
| Molecular Weight | High (( () | Moderate | Moderate |