MULTIDIMENSIONAL ORDER OF MACROMOLECULES

Molecular

Composition

Regioselectivity of monomer insertion

head to head vs head to tail

1,2 vs 1,4 addition

Stereochemistry of substituent placement

tacticity

chirality

Molecular weight and molecular weight 	distribution

Regularity of chain structure

linear, branched or crosslinked

Microscopic (Intermolecular Interactions)

crystallinity

phase separations - microdomains

chain ordering - liquid crystalline

Controlled by Intermolecular forces

Dispersion (Van der Waals) interaction

Dipolar association

Hydrogen bonding

Ionic bonding

Covalent bonding

Macroscopic Properties (Physical Behavior)

Tensile and/or Compressive Strength

Elasticity

Toughness

Thermal Stability

Flammability and Flame Resistance

Degradability

Solvent Resistance

Permeability

Ductility  (Melt Flow)

Surface Texture - - Morphology

Electrical and Optical Properties
Factors Controlling Morphology

Molecular Structure

(Monomer units, microstructures, molecular weight)

Conformation of
Single chain

Molecular Interactions

Rubberlike
Elasticity

Crystallite Formation

Glass Formation

% Crystallinity

Mechanical and Thermal Properties

Morphology

FACTORS REQUIRED TO PROMOTE CRYSTALLIZATION

Thermodynamic

1.  Symmetrical chains which allow regular close packing in crystallite

2.  Functional groups which encourage strong intermolecular attraction to stabilize ordered alignment.

Kinetic

1. Sufficient mobility to allow chain disentanglement and ultimate alignment

Optimum range for mobility

TM  -10(  (  Tg  + 30(

at TM  segmental motion too high

at Tg  viscosity too high

2. Concentration of nuclei

concentration of nucleating agents

thermal history of sample

GLASS TRANSITION, Tg

Definition:  The onset of seqmental motion of seqments with 				40-50 carbons atoms

Physical Change   Expansion of volume

Free volume required to allow segmental motion

Properties Affected

Specific Volume / Density

Specific Heat, Cp

Refractive Index

Modulus

Dielectric Constant

Permeability

Tg is an approximation

Depends upon measurement technique

Depends upon molecular weight

Polystyrene MW = 4000		Tg = 40(C

= 300,000	      = 100(

FACTORS INFLUENCING Tg

Tg is proportional to Rotational Freedom

For symmetrical polymers  	Tg, / Tm in (K ( 1/2

unsymmetical polymers				  ( 2/3

1. Chain flexibility

Silicone ( Ether ( Hydrocarbon ( Cyclic HC ( Aromatics

2. Steric Bulk of Substituents

Tg = -120(C		    5(C		  -24(C		  -50(C

Long side chains may act as plasticizers (C ( 6)

Tg = 	  -55(C			     88(C

Tg =  5(C		   100(C		     150(C

3. Molecular Symmetry

Asymmetry increases chain stiffness.

4. Polar Interactions increase Tg

Hydrogen bonding

5. Molecular Weight up to Critical Limit

6. Crosslinking

Reduces Segment Mobility