General Approaches to Polymer Synthesis

1.	Addition		Chain Growth

Polymerization of Vinyl Monomers

2. Ring Opening Polymerization

Heterocylics

Methathesis of Cyclic olefins

3. Condensation		Step Growth

Polymerization of A-B or AA/BB Monomers

4. Modification of Preformed Polymers

Polysaccharides

Peptides and Proteins

Synthetic Precursors

Current Strategies in Polymer Synthesis

Objectives:  Precise Macromolecular Design

1.	Control of:		Molecular Weight

Composition

Sequence of repeat units

Stereochemistry

- Versatility

Synthetic Methods

- Step-growth (Condensation) Polymerization

Mw/Mn ( 2

Statistical compositions and sequences

- Chain-growth (Addition) Polymerization

Mw/Mn > 1.5 ( 2.0 (

Statistical compositions and sequences

Little stereochemical control

Major Developments in the 1950-60's

- Living Polymerization (Anionic)

Mw/Mn (  1

Blocks, telechelics and stars available (Controlled molecular architecture)

Statistical Stereochemical Control

Statistical Compositions and Sequences

Severe functional group restrictions

- Ziegler-Natta (Metal-Coordinated) Polymerization

Stereochemical Control

Polydisperse products

Statistical Compositions and Sequences

Limited set of useful monomers, i.e. olefins

Additional Developments in the 1980's

- "Immortal" Polymerization  (Cationic)

Mw/Mn ( 1.05

Blocks, telechelics, stars

(Controlled molecular architecture)

Statistical Compositions and Sequences

Severe functional group restrictions

Under Development in the 1990's

- "Living" Free Radical Polymerization

Mw/Mn ( 1.05

Blocks, telechelics, stars

(Controlled molecular architecture)

Statistical Compositions and Sequences

Broad range of monomers available

- Single-Site Catalysis–Metal Coordinated II

Enhanced Stereochemical control

Variable stereochemistry in single molecule possible

Narrow molecular weight distributions

Improved control of copolymerization

8.	Genetic approaches via Modified Microorganisms

Monodisperse in MW

Monodisperse in Composition

Sequentially Uniform

Stereochemically Pure

Diverse set of functional groups possible

Types of Vinyl Polymerization

|  | Advantage | Disadvantage |
| --- | --- | --- |
| Bulk | Simple Equipment | Heat Buildup |
|  | Rapid reaction | Gel effect |
|  | Pure polymer isolated | Branching or crosslinking occurs |
| Solution | Good mixing | Lower molecular weight formed |
|  | Solution ready for application | Low polymerization rate |
|  |  | Solvent recovery required |
| Suspension | Low viscosity media | Removal of impurities |
|  | Direct bead formation |  |
| Emulsion | Low viscosity media | Coagulation required to recover polymer |
|  | High polymerization rate |  |
|  | High molecular weight product |  |
|  | High surface area latex | Latex stability |
| Inverse Emulsion Water in Oil media | Polymerization of water soluble monomers |  |
|  | Emulsion inversion promotes polymer dissolution |  |

# HIGH PRESSURE POLYETHYLENE

K. W. Doak, Encylopedia of Polymer Science, Vol. 6, 386-429 (1986)

Tubular Reactors with inner diameter of 2-6 cm and length of 0.5-1.5 km

Residence Time 0.25-2.0 min.  (linear velocity ( 10 m/sec)

Initiator:  Trace oxygen ( ( 300 ppm) plus alkyl peresters

Chain Transfer Agents: butane, isooctane, propene, propionaldehyde

Initial Temperature 140-180(C  Peak Temp. 300-325(C  Final Temp 250-275(C

Conversion: 15-20% per pass

Molecular Weights: 20,000-100,000; MWD = 3-20  density = 0.91-0.93 g/cm3

Production in 2002 ( 8 billion lbs.

Applications:  Film (60%)    Injection molding 10-15%,

Wire and Cable Insulation 5%   Extrusion Coatings 10%,

POLYSTYRENE

Commercial Processes:

1. Solution  	High purity "crystalline" general purpose resin

2. Suspension	Beads for insulation and ion-exchange resins

3.  Emulsion	ABS resins

Solution Process:

Solvent  Ethyl Benzene  2-30% to control viscosity

Initiators:  Thermal, BPO, AIBN

Conversion  60-90% depending upon reactor configuration

Molecular weight: 50-150,000; MWD = 2-4

Tg = 85(C

Brittle, Low Solvent Resistance, Poor Weatherability

About 7 billion lbs plastic resin and 2 billion lbs elastomers produced:

only 1/3 are homopolystyrene.

Applications: Injection molding, Extruded sheets, Expanded foams

Production in 1999  6.5 billion lbs.

Suspension (Pearl) Polymerization

| Process Type | Aqueous Phase | Monomers Used | Product |
| --- | --- | --- | --- |
| BEAD Polymer Soluble in Monomer | ( 1% Sol. Polymer Suspending Agents Cu++ Inhibitors | Styrene Methyl Methacrylate Vinyl Acetate | Clear Beads |
| POWDER Polmer Insoluble in Monomer | Suspending Agents Electrolytes | Vinyl Chloride Acrylonitrile Fluoroethylene | Opaque Beads or Powders |
| INVERSE Hydrocarbon Media | Monomer Initiator | Acrylamide Acrylic Acids | Beads ( Emulsions |

Media to monomer ratio ( 3-4:1

Initiator must be soluble in monomer

Initiation occurs in large (0.05-1.0 mm) monomer drop

( 107 radicals/droplet at stationary state

Equivalent to a "mini-bulk" polymerization

Aqueous (hydrocarbon) media provides good heat transfer

Good particle size control through agitation and dispersion agents

Control of porosity with proper additives and process conditions

Product easy to recover and transfer

Disadvantages:

Suspending Agents contaminate product

Removal of residual monomer necessary

Suspension Polymerization of Styrene

Aqueous Phase:  	16.6 Kg of H2O

0.24 kg  Ca3PO4

0.14 kg Na+ Naphthalene sulfonate

0.077 kg. 15% Sodium Polyacrylate

Monomer Phase	16.6 Kg. Styrene 
(0.5 kg Methacrylic Acid)

0.012 kg AIBN

0.006 kg Benzoyl Peroxide

0.015 kg tert-Butyl Perbenzoate

Temperature Program

(C

Hours

POLY(VINYL CHLORIDE) SUSPENSION PROCESSES

Porous Beads				Low Temperature

Water			180 pt					200 pt

Vinyl Chloride		100 pt					100 pt

Polyvinyl			   0.5						   0.02
	Alcohol, 80-90%

Sodium 			...0.03	Polyethylene oxide	   0.005
	Naphthalene Sulfonate

Lauroyl Peroxide 	  0.5		Diisopropyl 		   0.5

Percarbonate

Butane			   3.0		Decompress at 40-50% Conversion
							by removing 10% VCl

Conditions				8 hr at 52(C				8 hr at 40(C

75% of Poly(vinyl chloride) produced by suspension processes

10% by Pechiney Process

15% by Emulsion Processes

SUSPENSION POLYMERIZATION IN

NON-AQUEOUS MEDIA

Monomer Phase 	Conc. Aqueous Solution (40%

Monomers				Initiators

Acrylamide				Potassium Persulfate

Acrylic Acids				Hydrogen Peroxide

Vinyl Pyrrolidone			Redox Systems

Quaternary Ammonium Monomers

Suspending Media

Hydrocarbon solvents

Long Chain Alcohols

Freons

Supercritical CO2

Stabilizing Agents:  	Hydrophobic polymers containing
hydrophilic functional groups

Hydroxyethyl Cellulose

Poly(vinyl ether-co-maleic anhydride)

Sulfonate Polystyrene

Sorbitol Oleate

Hydrophobic Clays

Silanized Silica

Components of Emulsion Polymerization

Stages of Emulsion Polymerization

Phase I	Phase II		Phase III

Conversion

Rate, (P/(t

time

| Particles/ (/ml | Phase I | Phase II | Phase III |
| --- | --- | --- | --- |
| Micelles | 1017-1018 | 0 | 0 |
| Monomer Droplets | 1011 | 1010 | 0 |
| Polymer Particles | 0 | 1015 | 1015 |
| Micelles | Monomer Droplets | Radical Concentration |
| Size 25A( | Size 10,000A( |  |
| Surfactant Molecules, 130 | 2.7 106 |  |
| Monomer, 73 | 2.5 1010 |  |
| Water |  | 1013 radicals/ml. sec |

EMULSION POLYMERIZATION

Advantages:

High rate of polymerization

High molecular weights

Few side reactions 		High Conversion achieved

Efficient heat transfer

Low viscosity medium	Polymer never in solution

Low tendancy to agglomerate

Emulsified polymer may be stabilized and used directly

Disadvantages:

Polymer surface contaminated by surface active agents

Coagulation introduces salts	Poor electrical properties

Kinetics of Emulsion Polymerization (Smith-Ewart Theory)

Rp = kp [M]p [R.]aq	where:

[M]p = Conc. of monomer in polymer particle

[R.]aq = Conc. of radicals in continuous (aqueous) phase

= 1015  radicals/ml sec

In practice both of these concentrations are constant during most of the polymerization

Since the number of polymer particles, N = 1015 particles/ml

On average, each particle received a new radical every 100 sec.

One radical /particle allows only propagation

Addition of second radical results in rapid termination

( Each particle is growing 1/2 of time

At steady state:

Rp ( ( of particles/2   = N kp [M] / 2

Molecular weight (() ( ( of particles/ ( R. sec-1 = N kp [M] / Ri

If N increases then DP increases!

Most important variable  Number of particles, N

Depends upon:

1. Type and Concentration of Surfactant (Emulsifier)

conc ranges from 1 - 8% relative to [M]

Common surfactants:

Dodecyl sulfonate or carboxylate  (anionic)

Nonylphenol-ethylene oxide adducts (neutral)

Cationic surfactants are inhibitors!

2. Electrolyte Concentration

High salt conc. decreases efficiency of surfactant

3. Rate of radical generation

Redox systems most common

4. Temperature

As temp. increases; kp and N increase but [M] decreases

5. Type and Intensity of Agitation

Must maintain dispersion of monomer droplets

6. Monomer/water ratio   controls heat transfer capacity

Water must be dionized and degassed

POLYMERS PRODUCED USING EMULSION PROCESSES

Polymer					Applications

Styrene-Butadiene Rubber		Tires, Belting, Flooring,

Molded goods, Shoe soles, Electrical insulation

Butadiene-Acrylonitrile 	Fuel tanks, Gasoline hoses,

(nitrile rubber)	Adhesives, Impregnated paper, leather and textiles

Acrylonitrile-Butadiene-Styrene	Engineering plastics,

(ABS)		household appliances,

Automobile parts, Luggage

Polychloroprene				Tires, Wire coatings, Belting,

(neoprene rubber)				hoses, Shoe heels, Coated

fabrics

Polyacrylates					Water based latex paints

Poly(acrylic acid) 				Adhesives, Thickening

agents,

Poly(methacrylic acid)				Ionomers

Inverse Emulsion Process

Polyacrylamide				Thickening agents,

Flocculants

STYRENE-BUTADIENE "COLD" RUBBER  "GR-S"

Emulsion				By Weight		Based upon 100 pts monomer

Butadiene					140 g				70

Styrene					 60 g				30

Water				360-400 ml			100-200

Potasium Lauryl Sulfate		 10.2 g			 5.1

Sodium Phosphate (pH = 10)	  1.2 g			 0.08

Versene - Fe +3				  0.14 g			 0.07

FeSO4					..0.1 g			 0.05

p-Menthane hydroperoxide		  0.2 g			 0.10

HOCH2SO3- Na+			  0.3 g			 0.15

(Sodium formaldehyde sulfoxylate)

tert-Dodecyl Mercaptan		  0.3 g			 0.15

Reaction Temp = 5(C,   Time = 12 hr.

Shortstop with Inhibitors  Then remove residual monomers by steam stripping

Add antioxidants and antiozonants

Two step coagulation

20 % NaCl    ( Cream

5%  H2SO4  ( Crumb

Chemistry of Initiation